PRODUCT DATA SHEET

PRODUCT DATA SHEET

PRODUCT DATA SHEET

Chemlube Premium AW Hydraulic Oil

Chemlube Premium AW Hydraulic oils are high quality antiwear hydraulic fluids formulated from premium base stocks to provide superior water separation, antiwear protection, rust and thermal stability. Premium AW Hydraulic oils are recommended for use in a variety of high-pressure mobile and stationary hydraulic system utilizing vane, piston or gear pumps. Other suitable applications (of proper grade) include lubrication of machine tools, servo controls, metalworking equipment as light duty crankcase oils, circulating systems bearings/journal (anti friction) and gear cases. Chemlube Premium AW Hydraulic oils are recommended for the use in hydraulic equipment made by major manufactures, including Bosch, Eaton Vickers, Dennison Parker, Racine, Cincinnati Lamb, Lee-Norse and many others.

Meets Performance Requirements:

Eaton Vickers M-2950-S, 1-286-S3                                                   ISO 11158 (HM, HV)

Racine var vol. Vane pumps                                                              Cincinnati Lamb P-68, P-69 & P-70

DIN 51524, Part 2 and 3                                                                    ANSI/AGMA 9005-E02-RO

JCMAS P041 (HK)                                                                             ASTM D 6158 (HM, HV)

AIST 126, 127                                                                                    GM LS-2

Denison Parker HF-0, HF-1, HF-2                                                     SAE MS 1004 (HM, HV)

Bosch RE 90 220

PREMIUM AW HYDRAULIC OILS

TYPICAL PROPERTIES

| TEST | METHOD | AW 32 Code 20032 | AW 46 Code 20046 | AW 68 Code 20068 | AW 100 Code 20100 |
| --- | --- | --- | --- | --- | --- |
| API Gravity | ASTM D4052 | 34.0 | 32.7 | 31.9 | 30.4 |
| Viscosity, cSt @ 40° C | ASTM D445 | 30.0 | 44.7 | 67.3 | 101.17 |
| Viscosity, cSt @ 100° C | ASTM D445 | 5.5 | 6.9 | 8.7 | 11.43 |
| Viscosity Index | ASTM D2270 | 119 | 111 | 109 | 99 |
| Flash Point ° C(F) | ASTM D92 | 216(420) | 216(420) | 216(420) | 216(420) |
| Pour Point ° C | ASTM D97 | -30(-22) | -30(-22) | -30(-22) | -17 |
| Color | ASTM D1500 | L1.0 | L1.5 | L1.5 | L1.0 |
| Zinc, ppm | Spectrometer | 500 | 500 | 500 | 500 |
| Oxidation Stability | ASTM D943 Min. hrs | 6000 | 6000 | 5000 | 5000 |

NOTE: Values are typical only. Due to ongoing research, development and product improvement,

product formulas are subject to change without notice. Chemlube International cannot know all the uses and conditions to which this product may be subjected, therefore it is the user’s responsibility to ascertain that it is suitable for any intended use or application. Reviewed 02-01-22.