PRODUCT DATA SHEET

PRODUCT DATA SHEET

## PRODUCT DATA SHEET

### Chemlube Premium Gold Series

## SAE 20W-50 /API SP

Chemlube Premium Gold is a premium engine oil that is formulated for turbo-charged and naturally spirited gasoline, propane, natural gas engines in passenger car and light duty truck service. The Premium 20W-50 meets or exceeds the API SP classification. This oil is designed for use in U.S., European, and Japanese passenger cars, vans, sport utility vehicles and light duty trucks.

| Features | # Applications |
| --- | --- |
| - Meets or exceeds API Service SN. - Meets passenger car and light truck manufacturers warranty requirements. - Lubricates, cools, and protects turbo-charged high-revving engines that operate at high temperatures. - Protects the engine in controlling varnish, deposits, rust, corrosion, wear, and cleanliness. - Designed to flow at low temperatures to get to vital engine parts quickly. | - Passenger car and truck gasoline, propane, and natural gas engines specifying API service SN engine oils. - Maintains the warranty requirements for today’s passenger car and light duty trucks. - Reduces high temperature oxidation. - Energy-Conserving for improved fuel economy. API license number 2325 |

SAE 20W-50 API SP   TYPICAL PROPERTIES

Product Code 12050

TEST                                                METHOD                                  Typical

cSt @ 40oC                                     ASTM D445                            161.1

cSt @ 100oC                                   ASTM D445                              19.1

Viscosity Index                              ASTM D2270                             135

CCS Viscosity, cP @-15oC            ASTM 5293                             6500

Flash Point oC                                ASTM D92                                208

Pour Point oC                                 ASTM D97                                 -25

Color                                               ASTM 1500                              <3.5

Zinc, ppm                                       Spectrometer                             850

Phosphorus, ppm                           Spectrometer                            790

NOTE: Values are typical only. Due to ongoing research, development and product improvement, product formulas are subject to change without notice. Chemlube International can not know all the uses this product may be subject to so it is the user’s responsibility to ascertain

that it is suitable for an intended use or application.

Reviewed 02-01-22