## PRODUCT DATA SHEET

### Chemlube Premium Gold Series

## Synthetic API SP / ILSAC GF-6

Chemlube Premium Gold Synthetic Series are premium engine oils that are formulated for turbo-charged and naturally spirited gasoline, propane, natural gas engines in passenger car and light duty truck service.  Premium Gold Synthetic motor oils are formulated using all Group lll base oils and the latest additive technology to meet or exceed the API SP classification and also meet the requirements of ILSAC GF-6 and are Resource Conserving (RC).  This oil is designed for use in U.S., European, and Japanese passenger cars, vans, sport utility vehicles and light duty trucks.

| Features | # Applications |
| --- | --- |
| - Meets or exceeds API Service SP - Backwards compatible to API SN, SM, SL, SJ - Meets or exceeds ILSAC GF-6 requirements - Resource Conserving (RC) - Meets passenger car and light truck manufacturers warranty requirements - Lubricates, cools, and protects turbo-charged high-revving engines that operate at high temperatures - Protects the engine in controlling varnish, deposits, rust, corrosion, wear and cleanliness - Designed to flow at low temperatures to get to vital engine parts quickly | - Passenger car and truck gasoline, propane and natural gas engines specifying API service SP engine oils - Maintains the warranty requirements for today’s passenger car and light duty trucks specifying ILSAC GF-6 engine oils - Reduces high temperature oxidation - Resource-Conserving for improved fuel economy. - API License Certification no. is #2325 |

SYNTHETIC API SP / ILSAC GF-6

TYPICAL PROPERTIES

| TEST | METHOD | 0W-20 Code 10022 | 5W-20 Code 10524 | 5W-30 Code 10535 |
| --- | --- | --- | --- | --- |
| Viscosity @40° C cSt | ASTM (D445) | 42.81 | 42.81 | 62.1 |
| Viscosity @ 100° C cSt | ASTM (D445) | 8.10 | 8.14 | 10.9 |
| Viscosity Index | ASTM (D2270) | 165 | 167 | 169 |
| CCS Viscosity cP @-35° C | ASTM (D5293) | 5482 |  |  |
| CCS Viscosity cP @-30° C | ASTM (D5293) |  | 2901 | 4532 |
| Flash Point ° C | ASTM (D92) | 206 | 202 | 206 |
| Pour Point, ° C | ASTM (D97) | -48 | -45 | -42 |
| Noack Volatility | ASTM (D5800) | 11.8 | 10.2 | 10.0 |
| Color | ASTM (1500) | L3.5 | L3.5 | L3.5 |
| Zinc, ppm | spectrometer | 840 | 836 | 834 |
| Phosphorus, ppm | spectrometer | 780 | 770 | 773 |

NOTE: Values are typical only. Due to ongoing research, development and product improvement, product formulas are subject to change without notice. Chemlube International cannot know all the uses and conditions to which this product may be subjected, therefore it is the user’s responsibility to ascertain that it is suitable for any intended use or application. Reviewed 02-01-22