## PRODUCT DATA SHEET

### Chemlube Premium Gold Series Synthetic Blend

## API SP / ILSAC GF-6A

Chemlube Premium Gold Series Synthetic Blends are premium engine oils that are formulated for turbo-charged and naturally aspirated gasoline, propane, natural gas engines in passenger car and light duty truck service.  Premium Gold motor oils meet or exceed the API SP classification and also meet the requirements of ILSAC GF-6A and are Resource Conserving (RC).  This oil is designed for use in U.S., European, and Japanese passenger cars, vans, sport utility vehicles and light duty trucks.

| Features | # Applications |
| --- | --- |
| - Meets or exceeds API Service SP. - Meets or exceeds ILSAC GF-6A requirements. - Backwards compatible to API SN Plus, SN, SM and SL. - Meets passenger car and light truck manufacturers warranty requirements. - Lubricates, cools, and protects turbo-charged high-revving engines that operate at high temperatures. - Protects the engine in controlling varnish, deposits, rust, corrosion, wear and cleanliness. - Designed to flow at low temperatures reaching vital engine parts quickly. | - Passenger car and truck gasoline, propane and natural gas engines specifying API service SP engine oils. - Maintains the warranty requirements for today’s passenger car and light duty trucks specifying ILSAC GF-6A engine oils. - Reduces high temperature oxidation. - Resource-Conserving for improved fuel economy. - API License Certification no. is #2325. |

API SP / ILSAC GF-6A

TYPICAL PROPERTIES

| TEST | METHOD | 0W20 Code 10023 | 5W-20 Code 10521 | 5W-30 Code 10531 | 10W-30 Code 11032 | 10W-40 Code 11043 |
| --- | --- | --- | --- | --- | --- | --- |
| Viscosity cSt @ 40° C | ASTM (D445) |  | 51.69 | 64.95 | 64.1 | 108.4 |
| Viscosity cSt @ 100° C | ASTM (D445) |  | 8.9 | 10.9 | 10.2 | 15.9 |
| Viscosity Index | ASTM (D2270) |  | 154 | 158 | 146 | 157 |
| CCS Viscosity, cP @-35C | ASTM (D5293) |  | ------ | ----- |  |  |
| CCS Viscosity, cP @-30C | ASTM (D5293) |  | 5049 | 5840 |  |  |
| CCS Viscosity, cP @-25C | ASTM (D5293) |  | ------ | ------ | 5212 | 5475 |
| Flash Point ° C | ASTM (D92) |  | 200 | 200 | 202 |  |
| Pour Point ° C | ASTM (D97) |  | <-42 | <-42 | <-39 | <-35 |
| Noack Volatility | ASTM (D5800) |  | 11.0 | 11.9 | 9.1 | 8.7 |
| Color | ASTM (D1500) |  | L3.5 | L3.5 | L3.5 | L3.5 |
| Zinc, ppm | Spectrometer |  | 858 | 859 | 859 | 868 |
| Phosphorus, ppm | Spectrometer |  | 789 | 767 | 765 | 770 |

NOTE: Values are typical only. Due to ongoing research, development and product improvement, product formulas are subject to change without notice. Chemlube International cannot know all the uses and conditions to which this product may be subjected therefore it is the user’s responsibility to ascertain that it is suitable for any intended use or application. Reviewed 02-01-22.