PRODUCT DATA SHEET

Product Code 40001

Chemlube Multipurpose Automatic Transmission Fluid

Chemlube Automatic Transmission Fluid is an automatic transmission fluid formulated to meet the needs of high performance, multi-purpose, power transmission fluid requirements. It is designed for use in passenger car and light truck automotive transmissions.  It is a blend of high quality base oils and premium additives that provide outstanding oxidation and thermal stability, friction control, load-carrying ability, corrosion and wear protection as well as preventing the accumulations of deposits and the formation of sludge, varnish, and foam.  It is especially effective in reducing and minimizing annoying transmission “chatter”, and provides fast circulation during cold weather and excellent lubrication and performance when hot.

FEATURES AND BENEFITS:

- Universal unlicensed product that meets prior GM/Ford ATF standards.

- Allison C-4 and other applications calling for use of DlllH/M quality ATF.

- Provides quiet shifting. - Reduces wear of critical parts. - Reduces maintenance costs and extends transmission life. - Outstanding thermal stability and oxidation resistance. - Eliminates transmission noise and vibration. - Inhibits foaming. - Protects transmission against rust, corrosion and varnish TYPICAL PROPERTIES: Test Method Results Viscosity 100C cSt ASTM D445 7.34 Viscosity 40C cSt ASTM D445 36.07 Viscosity Index ASTM D2270 175 Pour Point, C ASTM D97 < -38 Phosphorus, ppm Spectrometer 240.

NOTE: Values are typical only. Due to ongoing research, development and product improvement, product formulas are subject to change without notice. Chemlube International cannot know all the uses and conditions to which this product may be subjected therefore it is the user’s responsibility to ascertain that it is suitable for any intended use or application.

Reviewed 02-01-22