PRODUCT DATA SHEET

Chemlube Synthetic MVATF

Product Code 40002

Product Description

Chemlube Synthetic MVATF is a synthetic universal automatic transmission fluid specifically designed for passenger car and light duty trucks to meet the performance requirements and suitability for use in the vast majority of today’s modern Fuel Efficient transmissions (6 or more speeds).  Its performance features can also be realized in the vast majority of older transmission applications (<6 speeds).

Product Features and Benefits

- Lower inventory cost; one ATF can be used for a vast majority of Automatic Transmissions on the road today.

- Longer equipment life; specially formulated for extra wear control, corrosion protection formation of lacquers, sludge or other harmful deposits.

- Smooth Operations; JASO 1A Anti Shudder Durability (ASD) Performance

- Designed for modern fuel efficient transmissions as well as older transmissions

- Designed for longer fluid life and faster oil flow in low temperature operation.

- Consistent shift quality throughout the life of the fluid.

- Improved performance vs. Dexron® III :

  - Friction Stability

  - Clutch Durability

  - Oxidation Resistance

  - Foaming Resistance

  - Wear Control

  - Corrosion Control

- Frictions modifiers control lock-up rates of clutch packs for proper transmission shifting characteristics and efficient power transfer.

- Controls seal deterioration to limit fluid leakage.

- Multi-graded for optimum performance during cold starts and high temperature operations, including start/stop severe service.

Dexron® is a registered trademark of General Motors

Typical Applications

| BMW/Mini | Isuzu | SAAB |
| --- | --- | --- |
| Chrysler/Dodge/Jeep | Jaguar | Toyota/Lexus/Scion |
| Ford/Mazda | Kia | Subaru |
| GM/Geo/Opel/Saturn | Land Rover | Suzuki |
| Honda | Mitsubishi | Volvo |
| Hyundai | Nissan/Infiniti/Renault | VW/Audi |
| Idemitsu | Porsche |  |

Exceptions:  		Non-planetary transmissions (e.g. CVT, DCT)

Fluid Exceptions: 	Type F/G, ZF Lifeguardfluid6 and ZF Lifeguardfluid8

Typical Properties

| API Gravity | ASTM D4052 | 35.6 |
| --- | --- | --- |
| Viscosity @40C, cSt | ASTM D445 | 31.8 |
| Viscosity @100C, cSt | ASTM D445 | 6.3 |
| Viscosity Index | ASTM D2270 | 153 |
| Brookfield Viscosity, cPs @-40C | ASTM D2983 | 11,240cP |
| Pour Point C | ASTM D97 | <-42C |
| Color | ASTM D5100 | Red |

Suitable for Use in the following applications:

| OEM | DESCRIPTION | CODE | OEM | DESCRIPTION | CODE | OEM | DESCRIPTION | CODE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BMW | P/N 83 22-2 163 514 | SL017 | Hyundai | ATF RED-1K | SL004 | Multiple | M-L12108 | SL093 |
|  | ATF 6 | SL158 |  | SP-III | SL042 |  | LT 71141 | AE |
|  | ETL-7045 | SL100 |  | SP-IV | SL043 |  | M-1375.4 | SL095 |
|  | ETL-7045 E | SL101 |  | SP-IV-RR | SL112 | Nissan | Fluid A | SL079 |
|  | P/N 83 22-0 024 359 | SL102 | Isuzu | Genuine ATF | SL045 |  | Matic D | SL080 |
|  | LA 2634 | SL094 | Jaguar | K17 | SL044 |  | Matic J | SL081 |
|  | M-L12108 | SL096 | JASO | M315-2013 1-A | JASO HV |  | Matic K | SL082 |
| FCA | ASRC | SL067 |  | M315-2013 1-A-LV | JASO LV |  | Matic S | SL083 |
|  | AW-1 | SL117 | Kia | SP-III | SL025 | Porsche | P/N 000 043 204 63 | SL087 |
|  | P/N 05127382AA | SL072 |  | SP-IV | SL046 |  | P/N 000 043 304 00 | SL142 |
|  | P/N 68218925AA | SL076 | Land Rover | AW-1 | SL077 | Saab | ATF HP | SL021 |
|  | SP-IV | SL164 |  | N402 | SL103 |  | ATF Z1 | SL111 |
|  | ATF SP-4 | SL153 | Mazda | ATF FZ | SL049 |  | P/N 93 165 147 | SL090 |
|  | P/N 68171866AA | SL107 |  | ATF M-V | SL050 | Subaru | P/N K0140Y0700 | SL097 |
|  | Type 7176E | AP3 | Mercedes | 3403 M115 | SL092 | Suzuki | Matic D | SL129 |
|  | Type 9602 | AP4 |  | Sheet 236.1 | SL053 |  | Matic J | SL098 |
| FORD | FNR5 | SL027 |  | Sheet 236.10 | SL054 |  | Matic S | SL099 |
|  | P/N XT-10-QLV | MLV |  | Sheet 236.10, .12 or .14 | SL131 | Toyota | JWS 3309 | TIV |
|  | P/N XT-2-QDX | MA |  | Sheet 236.12 | SL055 |  | JWS 3324 | WS |
|  | P/N XT-5-QM | MA5 |  | Sheet 236.14 | SL057 |  | Scion ATF FZ | SL166 |
|  | P/N XT-5-QSM | MA5S |  | Sheet 236.15 | SL058 |  | Type T | TTA |
|  | P/N XT-6-QSP | MSP |  | Sheet 236.41 | SL059 | Volvo | AW-1 | SL130 |
| GM | GM 6032M [D] GM 6137M [E] | AF2 |  | Sheet 236.6 | SL060 |  | P/N 31 256 774 | SL106 |
|  | GM 6417M [G] GM N10055 [H] | AF3 |  | Sheet 236.7 | SL061 | VW | VW G 052 025 | SL006 |
|  | GM W16444 | AF6 |  | Sheet 236.8 | SL062 |  | VW G 052 990 A2 | SL011 |
|  | P/N 19256039 | SL036 |  | Sheet 236.9 | SL064 |  | VW G 055 005 A2 | SL012 |
| Honda | ATF Type 3.0 | SL157 | Mitsubishi | ATF-J2 | SL024 |  | VW G 055 162 A2 or A6 | SL014 |
|  | ATF Type 3.1 | SL162 |  | ATF-J3 | SL108 |  | VW G 055 540 A2 | SL015 |
|  | ATF-Z1 | SL040 |  | SP-III | SL065 |  | VW G 060 162 A2 | SL016 |
|  | Honda ATF-DW-1 | SL001 |  |  |  |  | VW GUS 00 162 | SL144 |
|  | Honda ATF-Z1 | SL002 |  |  |  |  |  |  |

| CHRYSLER | MS 9602 (ATF+4®) | -- | 7.3 | 7.8 | -- | 10,000 max | 6.5 min. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| GM | DEXRON®-III(H) (1) | -- | -- | -- | -- | 20,000 max. | -- |
| GM | DEXRON®-VI | 32 max. | -- | 6.4 | 145 | 15,000 max. | 5.5 min. @40hr |
| FORD | MERCON® (1) | -- | 6.8 | -- | -- | 20,000 max. | -- |
| FORD | WSS-M2C938-A (2) | -- | -- | 6.2 | -- | 12,000 max. | 5.5 min (5.0@40hr) |
| FORD | MERCON® V | -- | 6.8 | 8.1 | -- | 13,000 max. | 6.0 min. |
| FORD | MERCON® SP | -- | 5.5 | 6.0 | -- | 9,500 max. | 5.0 min. |
| JASO | M315-2002 1A | -- | 5.7 | -- | 120 | 20,000 max. | 5.4 min (5.7 sonic) |
| VOITH | H55.6335 | -- | -- | 8.2 | -- | 20,000 max. | 5.3 min |
| VOITH | H55.6336 | -- | -- | 8.2 | -- | 20,000 max. | 5.3 min. |
| ZF | TE-ML 14A | -- | 7.0 | -- | -- | 20,000 max. | 5.3 min |
| ZF | TE-ML 14B | -- | 7.0 | -- | -- | 20,000 max. | 5.5 min |
| - Obsolete specification - MERCON® LV factory fill; service fill specification has not been published |  |  |  |  |  |  |  |

.

NOTE: Values are typical only. Due to ongoing research, development and product improvement, product formulas are subject to change without notice. Chemlube International cannot know all the uses and conditions to which this product may be subjected, therefore it is the user’s responsibility to ascertain that it is suitable for any intended use or application. Reviewed and revised 02-09-21